1995 CSI SECTION 08120 Aluminum Doors And Frames

2004 CSI SECTION 08 11 16 Aluminum Doors And Frames

Part 1 – General

- Summary

  - Section includes:

    - Aluminum Doors and Frames

  - Related Sections:

- References

  - American Architectural Manufacturers Association (AAMA)

  - American Society for Testing and Materials (ASTM)

  - Aluminum Association (AA)

- System Description

  - General: In addition to requirements shown or specified, comply with:

    - Applicable provisions of AAMA Aluminum Storefront and Entrance Manual for design, materials, fabrication and installation of component parts.

  - Design Requirements: Arcadia 450T Series Arena Entrance System is a single source package of door, doorframe and hardware that is engineered for monumental appeal and maximum protection in tough traffic areas.

  - Performance Requirements: Each assembly tested by a recognized testing laboratory or agency in accordance with specified test methods.

    - Tested by the dual moment corner joint strength test.

- Quality Assurance

  - Single Source Responsibility:

    - Obtain entrances, storefronts, ribbon walls, window walls, curtain walls, window systems, and finish through one source from a single manufacturer.

  - Provide test reports from AAMA accredited laboratories certifying the performances as specified in 1.03.

- Warranty

  - Door warranted against failure and/or deterioration of metals due to manufacturing process for a period of two (2) years.

Part 2 – Products

- Manufacturers

  - Acceptable Manufacturers:

    - Arcadia, Inc., 2301 E Vernon, Vernon, CA. Telephone 323/269-7300, Fax 323/269-7390.

  - Acceptable Products:

    - Arcadia, Inc., 450T Series, Arena Entrance System, 2-¼”.

      - Vertical Stiles: 6 inches.

      - Top Rail: 4-1/2 inches.

      - Bottom Rail: 10 inches.

      - Glazing Insert: Snap-in type for _______ (1/4” or 1”) infill.

    - Door stiles, rails and frames shall have a nominal .188” and inserts shall have a .062” wall thickness.

- Materials and Accessories

  - Door members: Extruded 6063-T6 aluminum alloy (ASTM B221-Alloy G.S. 10a T6).

  - Screws, fastening devices, and internal components: Aluminum, stainless steel, or zinc plated steel in accordance with ASTM A-164. Shall be aluminum or steel, providing the steel is properly isolated from aluminum.

  - Glazing Gasket (compression-type design).

- Hardware

  - Hardware furnished and installed by the door manufacturer, and include the following standard hardware (as selected).

    - Weatherstripping: Hard-backed poly pile in door and/or frame. Meeting stile of all pair of doors have a double line hard-backed poly-pile astragal.

    - Threshold: Extruded Aluminum with ribbed surface.

    - Sill Sweeps: Brush strip (exposed, concealed).

    - Pivoting/Hinging: (Center, offset pivot; butt, continuous.)

    - Closers: (Overhead concealed, surface, floor.)

    - Latches/Strike: (Dead-latch combination, two-point.)

    - Latch Handle: (Lever, eurostyle/ w/return, paddle.)

    - Electric Release: (Offset strike, center hung strike.)

    - Locks/Strike: (Maximum security hooklock, deadbolt.)

    - Auxiliary Locks: (Two-point, three-point, flushbolts.) Cylinders: (Mortise, rim, dummy, thumbturn.)

    - Panic Devices: (Cross, touch bar, flush mid panel.)

    - Push/Pulls: (Standard, offset radius, straight radius.)

    - Cylinder Guard: (Security ring/retainer ring.)

    - Exit Indicator: (Message panel.)

    - Transom Decal: (This door to remain . . . )

    - Door Stop/Holder:

    - Mail slot.

SPECIFIER NOTE: Refer to Arcadia Architectural Manual, Hardware Section for description of items 4-18.

- Finish

  - Finish all exposed areas of aluminum and components as indicated.

    - An Architectural Class II or I color anodic coating conforming with AA-M12C22A34/AA-M12C22A44.

      - Anodized finish color shall be Colornodic _____. (AB1 Light Champagne, AB2 Champagne, AB3 Light Bronze, AB4 Medium Bronze, AB5 Standard Medium Bronze, AB6 Dark Bronze, AB7 Standard Dark Bronze, AB8 Black.)

    - An Architectural Class II or I anodic coating conforming with AA-M12C22A31/AA-M12C22A41.

      - Anodize finish color shall be Colornodic ______ (#11 Clear)

    - Fluorocarbon Coating: AAMA 2605.2.

      - Resin: 70% PVDF Kynar 500/Hylar 5000.

      - Substrate: cleaned and pretreated with chromium phosphate.

      - Primer: Manufacturer’s standard resin base compatible coating. Dry film thickness.

        - Extrusion: Minimum 0.20 mil.

      - Color Coat: 70% PVDF, dry film thickness.

        - Extrusion: 1.0 mil.

      - Color: As selected by Architect.

      - Acceptable Coatings Manufacturers:

        - PPG Industries, Inc.

        - Valspar Corporation

        - BASF

- Door Fabrication

  - Door stiles and rails shall be tubular sections accurately joined at corners with heavy concealed thru bolts, machine bolts and then MIG welded.

  - Each door leaf equipped with an adjusting mechanism, located in the top rail near the lock stile.

  - Custom hardware templates and physical hardware must be submitted prior to any fabrication.

Part 3 – Execution

- Examinations

  - Examine conditions and verify substrate conditions are acceptable for product installation.

- Installation

  - Install in accordance with approved shop drawings and manufacturers installation instructions.

- Field Quality Control

  - Make all necessary final adjustments to attain normal operation of each door and its mechanical hardware.

END OF SECTION

# Text boxes

(or)

(or)