1995 CSI SECTION 08120 Aluminum Doors And Frames

2004 CSI SECTION 08 11 16 Aluminum Doors And Frames

Part 1 – General

- Summary

  - Section includes:

    - Aluminum Terrace Doors and Frames

  - Related Sections:

- References

  - American Architectural Manufacturers Association (AAMA)

  - American Society for Testing and Materials (ASTM)

  - Aluminum Association (AA)

- System Description

  - General: In addition to requirements shown or specified, comply with:

    - Applicable provisions of AAMA Windows and Sliding Glass Doors Manual for design, materials, fabrication and installation of component parts.

  - Design Requirements: Arcadia IPARC8250 Series Terrace Door is a single source package of door, doorframe and hardware that is engineered for hi-rise, condominiums and hotel applications.

  - Performance Requirements: Each assembly tested by a recognized testing laboratory or agency in accordance with specified test methods.

    - Conformance to ASTM 1886/1996 ( Small Missile & Large Missile ) & AAMA/NWWDA 101/I I.S. 2-97 ( Non Impact).

    - Water Penetration: No water leakage when tested per ASTM E 331 at a static air pressure difference of 6.24 psf.

    - Air Infiltration: Accordance with ASTM E 283 at a static air pressure difference of 6.24 psf. Air infiltration shall not exceed .30 cfm per square foot.

    - Uniform Structural: Door leaf to be operable when tested per ASTM E 330 at a static air pressure difference of 30 psf.

- Quality Assurance

  - Single Source Responsibility:

    - Obtain entrances, storefronts, ribbon walls, window walls, curtain walls, window systems, and finish through one source from a single manufacturer.

  - Provide test reports from AAMA accredited laboratories certifying the performances as specified in 1.03.

- Warranty

  - Aluminum terrace door and frame warranted against failure and/or deterioration of metals due to manufacturing process for a period of two (2) years.

Part 2 – Products

- Manufacturers

  - Acceptable Manufacturers:

    - Arcadia, Inc., 2301 E Vernon, Vernon, CA. Telephone 323/269-7300, Fax 323/269-7390.

  - Acceptable Products:

    - Arcadia, Inc., IPARC8250 Series Terrace Door and Frame

      - 3 1/4 frame depth.

      - 2 15/16” door leaf depth.

      - Configuration: Outswing; [inswing]; single [double] door leaf per frame.

      - Glazing Stops: Snap-in type for ________ (1/4  - 1 inch) infill.

- Materials and Accessories

  - Door members: Extruded 6063-T6 aluminum alloy (ASTM B221-Alloy G.S. 10a).

  - Screws, fastening devices, and internal components: Aluminum, stainless steel, or zinc plated steel in accordance with ASTM A-164. Shall be aluminum or steel, providing the steel is properly isolated from aluminum.

  - Glazing Gasket

    - Compression-type design.

2.03 Hardware

  - Hardware furnished and installed by the door manufacturer, and include the following standard hardware.

    - Weatherstrip: Secured in extruded ports; double rows on door leaf perimeters; compression bulb design.

    - Hinging: Butt hinge.

    - Latch Handle: Lever.

    - Locks: Multipoint door locking system.

- Finish

  - Finish all exposed areas of aluminum and components as indicated.

    - An Architectural Class II or I color anodic coating conforming with AA-M12C22A34/AA-MI2C22A44.

      - Anodized finish color shall be Colornodic _____. (AB1 Light Champagne, AB2 Champagne, AB3 Light Bronze, AB4 Medium Bronze, AB5 Standard Medium Bronze, AB6 Dark Bronze, AB7 Standard Dark Bronze, AB8 Black.)

    - An Architectural Class II or I anodic coating conforming with AA-M12C22A31/M12C22A41.

      - Anodize finish color shall be Colornodic ______ (#11 Clear)

    - Fluorocarbon Coating: AAMA 2605.2.

      - Resin: 70% PVDF Kynar 500/Hylar 5000.

      - Substrate: cleaned and pretreated with chromium phosphate.

      - Primer: Manufacturer’s standard resin base compatible coating. Dry film thickness.

        - Extrusion: Minimum 0.20 mil.

      - Color Coat: 70% PVDF, dry film thickness.

        - Extrusion: 1.0 mil.

      - Color: As selected by Architect.

      - Acceptable Coatings Manufacturers:

        - PPG Industries, Inc.

        - Valspar Corporation

        - BASF

- Door Fabrication

  - Frame: Head and sill fastened to jambs with four #12-24 x 3/4 inch screws per corner.

  - Door Leaf: Tubular horizontal door leaf rails mitered, reinforced with an extruded corner key, and welded.

  - All corners shall be weathersealed with an elastomeric sealant.

Part 3 – Execution

- Examinations

  - Examine conditions and verify substrate conditions are acceptable for product installation.

- Installation

  - Install in accordance with approved shop drawings and manufacturers installation instructions.

- Field Quality Control

  - Make all necessary final adjustments to attain normal operation of each door and its mechanical hardware.

END OF SECTION

# Text boxes

(or)

(or)