1995 CSI SECTION 08585 Security Screens

2004 CSI SECTION 08 5666 Security Screens

Part 1 – General

- Summary

  - Section includes:

    - Aluminum Operable Security Screens

  - Related Sections:

- References

  - American Architectural Manufacturers Association (AAMA)

  - American Society for Testing and Materials (ASTM)

  - Aluminum Association (AA)

- System Description

  - General: In addition to requirements shown or specified, comply with:

  - Design Requirements: Arcadia Intruder 175 Series designed to fit any fixed or operable Arcadia window product. Adams Rite 1841 dead bolt locking hardware with throw bolt for 3 point locking system

  - Performance Requirements:

    - Screens to meet a minimum Level 6 Security Level

- Quality Assurance

  - Single Source Responsibility:

    - Obtain Security Screens, entrances, storefronts, ribbon walls, window walls, curtain walls, window systems, and finish through one source from a single manufacturer.

Warranty

  - 2. System shall be warranted against failure and/or deterioration of metals due to manufacturing process for a period of two (2) years.

Part 2 – Products

- Manufacturers

  - Acceptable Manufacturers:

    - Arcadia, Inc., 3225 East Washington Blvd., Vernon, CA. Telephone 323/269-7300, Fax 323/269-7390.

  - Acceptable Products:

    - Arcadia, Inc., Intruder 175 Series

- Framing Materials and Accessories

  - Framing members, transition members, mullions, adaptors, and mounting: Extruded 6063-T6 aluminum alloy (ASTM B221 – Alloy G.S. 10a T6). Minimum .125” wall thickness on all framing members and .090” on all sash extrusions.

  - Perforated steel screen infill to be 14-gauge powder coated steel with an option for any type of woven mesh specified.

  - Screws, fastening devices, and internal components: Aluminum, stainless steel, or zinc-plated steel in accordance with ASTM.A-164. Perimeter anchors shall be aluminum or steel, providing the steel is properly isolated from aluminum. Provide tamper proof fasteners where  necessary

- Finish

  - Finish all exposed areas of aluminum and components as indicated.

    - An Architectural Class II or I color anodic coating conforming with AA-M12C22A34/AA-M12C22A44.

      - Anodized finish color shall be Colornodic _____. (AB1 Light Champagne, AB2 Champagne, AB3 Light Bronze, AB4 Medium Bronze, AB5 Standard Medium Bronze, AB6 Dark Bronze, AB7 Standard Dark Bronze, AB8 Black, AG2 Gold.)

    - An Architectural Class II and I anodic coating conforming with AA-M12C22A31/AA-M12C22A41.

      - Anodize finish color shall be Colornodic ______ (#11 Clear)

    - Fluorocarbon Coating: AAMA 2605.2.

      - Resin: 70% PVDF Kynar 500/Hylar 5000.

      - Color: As selected by Architect.

- System Fabrication

  - The perforated panel shall be attached between the main frame and interlocking cover plate with tamper resistant screws 3 inches on center maximum

  - There shall be no exposed fasteners at perimeter sections.

Part 3 – Execution

- Examinations

  - Examine conditions and verify substrate conditions are acceptable for product installation.

- Installation

  - Install in accordance with approved shop drawings and manufacturers installation instructions.

END OF SECTION

# Text boxes

(or)

(or)