SECTION 08520 ALUMINUM WINDOWS

Part 1 – General

- Summary

  - Section includes:

    - Aluminum Windows

  - Related Sections:

- References

  - American Architectural Manufacturers Association (AAMA)

  - American Society for Testing and Materials (ASTM)

  - Aluminum Association (AA)

  - California Association of Window Manufacturers (CAWM)

- System Description

  - General: In addition to requirements shown or specified, comply with:

    - Applicable provisions of AAMA Windows and Sliding Glass Doors Manual for design, materials, fabrication and installation of component parts.

  - Design Requirements: Arcadia Series C3100 AW-PG90-FW Thermal Fixed Window.

  - Performance Requirements: Each assembly tested by a recognized testing laboratory or agency in accordance with specified test methods. Air, water and structural test unit sized and configuration shall conform to requirements set forth in ANSI/AAMA 101-93

    - Conformance to AAMA 101/I.S. 2-97.

      - Air Infiltration: Test unit in accordance with ASTM E 283-04 at a static air pressure difference of 6.24 psf. Air infiltration shall not exceed .02 cfm per square foot.

      - Water Resistance: Test unit in accordance with ASTM E 547 & 331-00 at a static air pressure difference of 12.0 psf. No water leakage.

      - Uniform Load Structural: Tested per ASTM E 330-02 and ASTM 547 at a static air pressure difference of 135 psf.

      - Uniform Load Deflection: Tested per ASTM E 330-02 @3120 Pa Interlock (90 psf).

      - Component testing: Test unit in accordance with procedures described in AAMA 101/I.S. 2-97.

      - Forced Entry Resistance: Conform to ASTM F 588-07 Grade 40: No Entry.

      - Condensation Resistance Factor (CRF): Test unit in accordance with AAMA 1503.1-88, the condensation resistance factor shall not be less than 56 for the frame, 64 for the glass.

      - Thermal Transmittance Test: Test unit in accordance with AAMA 1503.1-88 (U-Value) not more than .56 BTU/hr/sf/ºF.

      - Thermal Movements: Allow thermal movement resulting from the following maximum change (range) in ambient temperature.

        - 120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

- Quality Assurance

  - Single Source Responsibility:

    - Obtain entrances, storefronts, ribbon walls, window walls, curtain walls, window systems, and finish through one source from a single manufacturer.

  - Provide test reports from AAMA accredited laboratories certifying the performances as specified in 1.03.

- Warranty

  - Warranted against failure and/or deterioration of metals due to manufacturing process for a period of two (2) years.

Part 2 – Products

- Manufacturers

  - Acceptable Manufacturers:

    - Arcadia Inc. 3955 E. Craig Road Las Vegas, NV. 89030 702/944-4680, fax 702/951-2525.

  - Acceptable Products:

    - Arcadia Inc. C3100 Series Fixed Window.

- Materials

  - Extruded aluminum profiles 6063-T6 alloy and temper (ASTM B221 G.S. 10A-T5).

  - All framing members .062 minimum wall thickness.

  - Back glazing two-sided adhesive, 15 lbs./ft.3 density, polyethylene tape. Glazing wedges EPDM or Santoprene.

  - Thermal barrier material poured in-place two part polyurethane.

- Finish

    - An Architectural Class II or I color anodic coating conforming with AA-M12C22A34/AA-M12C22A44.

      - Anodized finish color shall be Colornodic _____. (AB1 Light Champagne, AB2 Champagne, AB3 Light Bronze, AB4 Medium Bronze, AB5 Standard Medium Bronze, AB6 Dark Bronze, AB7 Standard Dark Bronze, AB8 Black.)

    - An Architectural Class II or I anodic coating conforming with AA-M12C22A31/AA-M12C22A41.

      - Anodize finish color shall be Colornodic ______ (#11 Clear)

    - Fluorocarbon Coating: AAMA 2605.2.

      - Resin: 70% PVDF Kynar 500/Hylar 5000.

      - Substrate: cleaned and pretreated with chromium phosphate.

      - Primer: Manufacturer’s standard resin base compatible coating. Dry film thickness.

        - Extrusion: Minimum 0.20 mil.

      - Color Coat: 70% PVDF, dry film thickness.

        - Extrusion: 0.20 mil.

      - Color: As selected by Architect.

      - Acceptable Coatings Manufacturers:

        - PPG Industries, Inc.

        - Valspar Corporation

        - BASF

- Fabrication

  - Frame components shall be mortised and tightly joined using two (2) #8 stainless steel screws per joint.

Part 3 – Execution

- Examinations

  - Examine conditions and verify substrate conditions are acceptable for product installation.

- Installation

  - Install in accordance with approved shop drawings and manufacturers installation instructions.

- Field Quality Control

  - Contractor’s responsibility to make all necessary final adjustments to attain normal operation of each window and its mechanical hardware.

END OF SECTION

# Text boxes

(or)

(or)