1995 CSI SECTION 08520 Aluminum Windows

2004 CSI SECTION 08 51 13 Aluminum Windows

Part 1 – General

- Summary

  - Section includes:

    - Aluminum Windows

a. 	Arcadia Inc., T325 Series (Thermal) Heavy Commercial Fixed, Casement, Awning and Hopper Windows, 3-1/4-inch depth.

  - Related Sections:

- References

  - American Architectural Manufacturers Association (AAMA)

  - American Society for Testing and Materials (ASTM)

  - Aluminum Association (AA)

  - National Wood Window & Door Association (NWWDA)

  - California Association of Window Manufacturers (CAWM)

- System Description

  - General: In addition to requirements shown or specified, comply with:

    - Applicable provisions of AAMA Windows and Sliding Glass Doors Manual for design, materials, fabrication and installation of component parts.

  - Design Requirements: Arcadia T325 Series (thermal) Heavy Commercial Fixed, Casement, Awning and Hopper Windows 3-1/4-inch depth. Hinged compression sealed aluminum windows. Suitable for outside or inside glazing.

  - Performance Requirements: Each assembly shall be tested by a recognized testing laboratory or agency in accordance with specified test methods.

    - Conformance to F-AW65, C-AW50, AP-AW40 specifications in AAMA/NWWDA 101/I.S. 2/A440-8.

      - Air Infiltration: Accordance with ASTM E 283 at a static air pressure difference of 6.24 psf. Air infiltration shall not exceed .30 cfm per square foot.

      - Water Resistance: Accordance with ASTM E 331/ASTM E 547 at a static air pressure difference of 12 psf. No water leakage.

      - Uniform Load Structural: Aluminum window systems comply with AAMA/WDMA/CSA 101/I.S.2/A440-08, Voluntary specifications for aluminum windows.  Guidelines for specified AW rated product.

      - Component testing: Accordance with procedures described in AAMA/NWWDA 101/I.S. 2/A440-08.

      - Forced Entry Resistance: All windows shall conform to CAWM 301-90 and ASTM F588-14.

      - Condensation Resistance Test: (CRF) in accordance with AAMA 1503.

      - Thermal Transmittance Test in accordance with AAMA 1503.

      - Thermal Movements: Allow thermal movement resulting from the following maximum change (range) in ambient temperature.

        - 120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

- Quality Assurance

  - Single Source Responsibility:

    - Obtain entrances, storefronts, ribbon walls, window walls, curtain walls, window systems, and finish through one source from a single manufacturer.

  - Provide test reports from AAMA accredited laboratories certifying the performances as specified in 1.03.

- Warranty

  - Warranted against failure and/or deterioration of metals due to manufacturing process for a period of two (2) years.

Part 2 – Products

- Manufacturers

  - Acceptable Manufacturers:

    - Arcadia, Inc., 2301 E Vernon, Vernon, CA. Telephone 323/269-7300, Fax 323/269-7390.

  - Acceptable Products:

    - Arcadia Inc., T325 Series (Thermal)

- Materials

  - Extruded aluminum profiles 6063-T6 alloy and temper (ASTM B221 G.S. 10A-T6).

  - All framing members .125 minimum wall thickness.

  - At Casement, Awning, and Hopper windows provide heavy-duty four bar hinges shall be stainless steel only, with asymmetric end caps, and adjustable limit stops. Lock and latches cast white bronze, US-25D finish.

  - Weatherstrip EPDM bulb type conforming to ASTM D2000 AA515 and shall be keyed into extruded grooves.

  - Back glazing two-sided adhesive, 15 lbs./ft.3 density, polyethylene tape. Glazing wedges shall be EPDM or Santoprene.

  - At operable windows provide screens made of extruded aluminum frame and screened with either 18 x 14 aluminum or fiber mesh.

  - Thermal barrier material poured-in-place two part polyurethane.

- Finish

    - An Architectural Class II or I color anodic coating conforming with AA-M12C22A34/AA-M12C22A44.

      - Anodized finish color shall be Colornodic _____. (AB1 Light Champagne, AB2 Champagne, AB3 Light Bronze, AB4 Medium Bronze, AB5 Standard Medium Bronze, AB6 Dark Bronze, AB7 Standard Dark Bronze, AB8 Black.)

    - An Architectural Class II or I anodic coating conforming with AA-M12C22A31/AA-M12C22A41.

      - Anodize finish color shall be Colornodic ______ (#11 Clear)

    - Fluorocarbon Coating: AAMA 2605.2.

      - Resin: 70% PVDF Kynar 500/Hylar 5000.

      - Substrate: cleaned and pretreated with chromium phosphate.

      - Primer: Manufacturer’s standard resin base compatible coating. Dry film thickness.

        - Extrusion: Minimum 0.20 mil.

      - Color Coat: 70% PVDF, dry film thickness.

        - Extrusion: 0.20 mil.

      - Color: As selected by Architect.

      - Acceptable Coatings Manufacturers:

        - PPG Industries, Inc.

        - Sherwin Williams

- Fabrication

  - Frame components mitered, reinforced extruded corner key, hydraulically crimped, and “cold welded.”

  - All ventilator extensions tubular, each corner mitered, reinforced extruded corner key, hydraulically crimped, and “cold welded.”

  - All corners weather sealed with an elastomeric sealant.

Part 3 – Execution

- Examinations

  - Examine conditions and verify substrate conditions are acceptable for product installation.

- Installation

  - Install in accordance with approved shop drawings and manufacturers installation instructions.

- Field Quality Control

  - Contractor’s responsibility to make all necessary final adjustments to attain normal operation of each window and its mechanical hardware.

END OF SECTION

# Text boxes

(or)

(or)